## Slide 1: Dillinger – BOF Steelmaking Automation & environmental aspects
Dominik Schöne

## Slide 2: Dillinger Hütte – an integrated metallurgical plant
Steel plant
Rolling mill
Coking plant
Blast furnace

## Slide 3: Dillinger Hütte – Steel plant

## Slide 4: Layout of the steel plant and production facilities
Hot metal D S
D P
D C
(rough adjustment
of temperature)
steel D S
D N
D H
(D C)
cleanliness
inclusion modification
cleanliness
prevention of resulphurization
minimization of segregation
prevention of surface defects
1 Hot metal re-ladling and desulphurization facility
2 Scimming facility 1 + 2
3 Top blowing BOF with bottom stirring 1 + 2
4 Ladle stirring stand / alloying stand
5 Gas injection stand
6 Tank degasser VD1/4
7 Tank degasser VD2/3
8 Continuous caster No. 4
9 Continuous caster No. 3
10 Continuous caster No. 5
11 Continuous caster No. 6
12 Ingot casting stand
Hot Metal
Converter Process
Secondary Metallurgy
Casting
1
2
3
3
4
4
5
5
6
7
8
9
10
11
12

## Slide 5: Content
Environmental aspects (Reducing Dust Emissions)
Steelmaking Automation (Sub Lances, Off-gas analysis, Slag carry over control, Ladle level control)

## Slide 6: BOF – primary dedusting system
BOF vessel ([C]-oxidation to CO/CO2); reducing dust emissions by adapting O2-flow rate
Primary dedusting system (Fe-oxide+lime dust, post-combustion CO to CO2 by surrounding air  steam generation in the boiler system)
2 lance systems for each BOF
Venturi system (water and steam flow)
Electric filter
Surrounding air (open system)
Tapping weight (t) 195
Volume (m³) 160
Specific volume (m³/t) 0,82
Bath depth (m) 1,65
6-hole lance (°) 17,5
Bottom porous plugs 6
max. 5 m³ i.N./min
Off gas analysis

## Slide 7: BOF – secondary dedusting system (SVAI)
Lime unloading and alloying bins (2009)
Air flow: 340.000 m3/h
Power ID fan: 1.000 kW
Dust: < 10 mg/Nm3
Filter house
BOF1&2 (Charging, tapping; 2010)
Air flow: 1.600.000 m3/h
Power ID fan: 2x2.500 kW
8 heat exchanger
Dust: < 10 mg/Nm3
+ secondary dedusting for hot metal reladling (430.000 Nm3/h) and deslagging

## Slide 8: Charging of scrap
Without secondary dedusting
With secondary dedusting

## Slide 9: Charging of hot metal
Without secondary dedusting
With secondary dedusting

## Slide 10: Automation: Control of BOF process
Charging
Online heat and time scheduler
Model for heat and mass balances
Lime calculation model
End of blow detection by off gas analysis
Dynamic control of lance height
Slagmon system for slag detection during tapping (possible: automatic end of tapping)
Dynamic control of bottom stirring
Temperature model (BOF and ladle)
Model for ladle desoxidation, lime and alloying
Temperature & sample manipulator (after blow; under construction)
Bath level control by radar (min. 1 per shift)
Ladle level control by laser measurement (VD, 1 per heat)

## Slide 11: Off gas analysis on the roof
End of blow if [C]-content is reduced to nearly 0.  EoB criteria: combination of t, %CO, %CO2, %O2; no sublance.
Charging

## Slide 12: Slag detection by Slagmon system (Primetals)
If slag is detected by IR during tapping: slag alarm and tilting of the vessel (manually); automatic end of tapping possible, but not in operation
Charging
a) Tapping of steel
b) Discharging of slag

## Slide 13: Temperature and sample manipulator (Primetals)
Already installed at BOF#2 (Sep 2019), but not yet in operation.
Charging